**CABRI 628 URINAL – MODESTY PANELS**
In Cabrillant toughened safety glass (ESG) as per EN 12150-2. Float 10 mm, entire surface enamelled using screen printing process, all edges polished smooth. Colours as per standard colour range.
Size 45 x 90 cm.

Wall fixing of urinal modesty panel using two double angle brackets.
No visible screw fittings.

Construction parts:

All connecting elements in aluminium (DIN 1725) are 100% corrosion-resistant and environmentally friendly. 100% recyclable.

Enamelled safety glass:

Enamels are lead- and cadmium-free, 100% recyclable.